Design, Optimization and Manufacturing of a Novel Corrugated Composite for Morphing Applications

Amirhosein Darbandi1*, Mohammad hossein Alaei2

1- Composite Materials and Technology Center, MalekAshtar University of Technology, Tehran, Iran.

2- Composite Materials and Technology Center, MalekAshtar University of Technology, Tehran, Iran.

* P.O.B. 1774-15875 Tehran, Iran, amirhosseindarbandi93@gmail.com

Abstract

In this study, a morphing airfoil consisting of corrugated composite core and Shape Memory Alloy (SMA) wire has been designed and optimized. For that reason, at first different corrugated GFRP composite structures having various shapes, pitch and thickness were designed and optimized to have morphing angle of 20 degrees, the lowest weight and maximum vertical displacement at the free end using the Responsive Surface Method (RSM). The analysis was done using the Abaqus software. In the next step the optimum corrugated GFRP composite structures determined by the RSM method in Design-Expert software was modeled in Abaqus. The optimum sample was then manufactured using a Foam mold and hand layup process. A nitinol SMA wire was used to actuate the manufactured corrugated structure. Finally the performance of the optimum model and manufactured sample was compared. The results showed that the triangular corrugated shape with 33.3 mm pitch and 0.48 mm thickness is the optimum sample having the minimum weight of 6.98 grams and maximum vertical displacement at the free end of 26.82 mm with morphing angle of 20 degrees. Comparing the displacement at the end of the numerical model and the manufactured sample shows a negligible difference of 1.42% showing a promising model to be used for further investigations in this area of research.

Keywords

Corrugated composite, Morphing airfoil, Shape Memory Alloy, Smart composite, Optimization

Introduction

Corrugated structures have wide application in engineering due to their special characteristics such as anisotropic behavior, high stiffness to weight ratio and high capacity of energy absorption. These structures have high industrial applications such as in packing industries, civil, Marine, aerospace and aeronautics. Among the aerospace applications of corrugated structures one can refer to the wings of morphing aircraft [1].

Composites are demanding materials that are being replaced by traditional materials due to their high superior properties [2]. Among the applications of composite materials is the corrugated composite structures. It is due to the importance of these structures that a high amount of research has been done in this area. Among these studies, one can refer to the study of Yokozeki et al. [3] where they developed a simple analytical model in order to predict the longitudinal and transverse stiffness of the corrugated composites. Kress and Winkler [4] derived an analytical expressions for an equivalent orthotropic plate of a corrugated sheet having circular patterns. Their model was capable of determining the stiffness matrices of a substitute plate with the same structural properties as the corrugated laminate. Thill et al. [5] studied the influence of the laminate thickness, geometry and fiber material on the stiffness of trapezoidal corrugated sheets. Dayyani et al. [6] proposed numerical and analytical solutions for the modelling of composite corrugated cores under tensile and three-point bending tests and reported that the mechanical behaviour of the core in tension is sensitive to the variation of core height. Ghabezi and Golzar [7] presented the effective stiffness in the longitudinal and transverse directions of various composite corrugated structures [8].

Several research studies on morphing structures using corrugated composite structures has been conducted [9, 10]. Yokozeki et al. [11] manufactured a variable camber morphing wing prototype using two servomotors that were used as actuators system to control the airfoil. Also Dayyani et al. [12] proposed the design of an elastomer coated corrugated skin for the camber morphing airfoil.

Some studies focused on combination of SMA and corrugated structures to form shape memory composites. For example, Ansari et al. [13] actuated  the corrugated composite beam by shape memory alloy wire. Talebi et al .[14] Carried out an experimental study on nonlinear response of trapezoidal corrugated composite panels actuated by SMA wires in the transverse direction. Koudzeri et al. [15] Studied the deflection of corrugated composite reinforced by shape memory alloy sheets by analytical and numerical methods.

For the shape control of flexible structures, SMA wires can be used as actuators in two types of embedded [16-18] and externally mounted [19-21]. In both types, the offset distances from the neutral axis of the beam produce the bending moment required for deforming the structure.

In this study, the effect of corrugated shape, pitch and thickness, has been investigated and optimized for minimum weight, maximum vertical displacement at the free end and morphing angle of 20 degrees for the first time in GFRP corrugated composite structure numerically. The performance of the optimum sample was then compared numerically and experimentally.

Method

2.1 Design of Experiments

Design of experiments is used to observe the effect of the input variables of a system or process on the response variables are measured it is applicable to both physical processes and computer simulation models [22]. One of the methods for design of experiments is the response surface methodology (RSM). This method is used to achieve breakthrough improvements in product quality and process efficiency and helps in carrying out less number of experiments while maintaining most important information [23].

The parameters of corrugation shape, pitch and thickness are three main parameters that effect the performance of the corrugated composite [7, 8]. It is for that reason that these parameters are chosen as input in this study and parameters like morphing angle, weight and maximum vertical displacement at the free end were chosen as output. The chosen input parameters are shown in Table (1).

TABLE I   Input parameters chosen in this study

| Levels |  |  | Factors |
| --- | --- | --- | --- |
| triangular | rectangular | sinusoidal | corrugation shape |
| 5 layers | 4 layers | 3 layers | thickness |
| 40 mm | 30 mm | 20 mm | pitch |

The RSM method in Design-Expert software was used for the optimization of these parameters. In order to have a high accurate model, the full factorial analysis was chosen for the experiments with overall 27 experiments. The designed experiments by the Design-Expert software is shown in Table (2).

TABLE II THE DESIGNED EXPERIMENTS

| No. of Experiments | Corrugation Shape | Thickness (mm) | Pitch (mm) |
| --- | --- | --- | --- |
| 1 | triangular | 0.64 | 40 |
| 2 | rectangular | 0.64 | 30 |
| 3 | triangular | 0.48 | 30 |
| 4 | triangular | 0.64 | 20 |
| 5 | rectangular | 0.64 | 20 |
| 6 | sinusoidal | 0.8 | 30 |
| 7 | rectangular | 0.64 | 40 |
| 8 | sinusoidal | 0.48 | 40 |
| 9 | sinusoidal | 0.64 | 40 |
| 10 | triangular | 0.48 | 20 |
| 11 | sinusoidal | 0.64 | 20 |
| 12 | sinusoidal | 0.48 | 20 |
| 13 | sinusoidal | 0.8 | 20 |
| 14 | sinusoidal | 0.8 | 40 |
| 15 | rectangular | 0.8 | 20 |
| 16 | triangular | 0.8 | 40 |
| 17 | triangular | 0.64 | 30 |
| 18 | rectangular | 0.48 | 40 |
| 19 | triangular | 0.8 | 20 |
| 20 | rectangular | 0.8 | 30 |
| 21 | sinusoidal | 0.48 | 30 |
| 22 | triangular | 0.8 | 30 |
| 23 | sinusoidal | 0.64 | 30 |
| 24 | rectangular | 0.8 | 40 |
| 25 | triangular | 0.48 | 40 |
| 26 | rectangular | 0.48 | 20 |
| 27 | rectangular | 0.48 | 30 |

  - Numerical Modeling

Since performing of all experiments (27 experiments) is expensive and time consuming, numerical modeling using FEM and Abaqus software was used. For this purpose at first the geometry of the corrugated composite was modeled according to Table (2) for each experiment. The cross section of the airfoil used was according to NACA 0012 due to its suitability to be used as morphing structure [24]. The length of the airfoil is assumed to 200 mm and width of 50 mm. Figure (1) shows the airfoils having different geometry and pitch. As it can be observed, in all of the geometries, the front side by 50 mm and the end by 30 mm has been fixed while the middle of the structure adjusted according to Table (1).

Fig 1 The various corrugation shapes and pitches used in modelling the core of airfoil

Later the material properties of the GFRP model was assigned according to Table (3). For obtaining of these properties, the GFRP composite plate was manufactured using the hand layup process and cut according to the ASTM D3039 (Figure (2)) for tensile testing of composite materials and finally tested using the Santam universal testing machine. The thickness of each composite layer was 0.16 mm with density of 1.9 kg/m 3 and 0.57 Volume of reinforcement. The type of model chosen was Elastic and Lamina.

Fig 2 The manufactured tensile samples

TABLE III The MECHANICAL PROPERTIES of The GFRP USED

| Material Properties | Value | Unit |
| --- | --- | --- |
| E11 | 25 | GPa |
| E22 | 25 | GPa |
| G12 | 4.5 | GPa |
| G23 | 4 | GPa |
| ν12 | 0.3 |  |

Meshing was done using the S4R element. This element is based on the first-order shear deformation theory, in which it is assumed that the shear strain is constant along the thickness. Constant thickness makes this element suitable for large rotations, reduced integral formulation and large strains. Figure (3) shows the meshed model of experiment number 8. The boundary condition used for the analysis consisted of one side fully fixed and another side free as shown in Figure (4).

Fig 3 Mesh model for corrugated composite

Fig 4 Boundary condition of corrugated composite

In order to model the force exerted by the SMA wire inside the Abaqus software, instead of modeling the SMA wire inside the software which is very complicated, the equivalent force measured from the actual SMA wire attached to the Santam universal testing machine and actuated by a heat torch was measured (Figure (5)) and entered inside the software as an concentrated load as shown in Figure (6). The value of this measured load was 80 N and the direction was tangent to the profile of the airfoil.

Fig 5 Measuring the equivalent load of the SMA wire

Fig 6 The equivalent 80N load applied on the two side of the model

After running the simulation, the response of the designed experiments including the vertical displacement and morphing angle were extracted from the Abaqus software and entered in the Design-Expert software in order to analyse the effect of input parameters on the output and to determine the optimum value.

  - Design optimization

After entering the response of the experiments, using the optimization module of Design-Expert software the effect of input parameters on the output was analysed and the optimum value of inputs were determined. The P-value for all three outputs were shown to be <0.0001 (significant) as the prove of appropriate optimization procedure (P-value of <0.005 is a sign of appropriate analysis). Also the R-squared for the vertical displacement, morphing angel and weight was reported as 0.98, 0.97 and 0.99.

  - Experimental and Numerical analysis of the optimum sample

The same procedure was taken for numerical modelling of the optimum sample in order to compare with the actual morphing airfoil. As for manufacturing of the optimum corrugated GFRP sample, Epikote 828 epoxy and Epikure F205 hardener was used as the matrix as a ratio of 100 to 50 along with the 200 gr/m E-glass fabric. Overall 3 layers of the fabric was used to approximately achieve 0.48 mm thickness by hand layup process as proposed by the Design-Expert software. A two sided foam mold (in order to achieve smooth surface on both side of the composite structure) was cut according to the pattern proposed for optimum sample. Figure (7) shows the steps taken for manufacturing of the corrugated GFRP composite.

The SMA used was a 1.5 mm nickel-titanium wire from Confluent ltd. With the commercial trade name of SM495. The wire was trained using the fixture shown is Figure (8-A) and the torch at the temperature limit of 500 to 550℃ as proposed by the supplier catalogue and finally attached to the composite structure by using of a nut and bolt. The final smart corrugated composite is shown in Figure (8-B)

Fig 7 Prepration of the foam mold (A), sample manufactering (B) and  final corugated sample produced (C)

Fig 8 Training of the SMA wire (A) and final smart corrugated composite (B)

Results and Discussions

The optimization was done with the goal of achieving max deformation, in order to use a lighter SMA wire, and the need for a lesser force to actuate the structure (Figure (9-A)). Weight was put to minimum since this factor is a main concern while designing any aircraft (Figure (9-B)). The morphing angle was put to 20 degrees since in a majority of aircrafts their flap angle is adjusted to be max 20 degrees after which the drag force increases exponentially after that (Figure (9-C)) [25].

The optimum input values proposed by the Design-Expert software is shown in Table (4). Among these optimum parameter combinations, number 1 was chosen as the optimum condition due to its higher desirability (0.653).

Figure (10) shows the result of numerical modeling of the optimum sample. As it can be observed, the max deformation is at the free end of the corrugated structure and the value is shown to be 2.76 cm.

Figure (11) shows the manufactured sample before (Figure (11-A)) and after actuating the SMA attached to the corrugated structure (Figure (11-B) by applying the current of 20 A for 6 seconds. The difference of position of the free end of the structure before and after actuating was measured using a roller to be 2.8 cm.

Fig 9 Optimization process for (A) max displacement, (B) minimum weight and (C) morphing angle of 20 degrees.

Table IV OPTIMUM COMBINATIONS of INPUT PARAMETERS PROPOSED by DESIGN-EXPERT SOFTWARE

| Number | Thickness (mm) | Pitch (mm) | Type | Displacement (mm) | Angle (degrees) | Weight (grams) | Desirability |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.48 | 33.339 | triangular | 26.823 | 20 | 6.98 | 0.653 | Selected |
| 2 | 0.48 | 35.522 | sinusoidal | 26.873 | 20 | 7.092 | 0.652 |  |
| 3 | 0.546 | 40 | rectangular | 27.98 | 20 | 9.954 | 0.602 |  |
| 4 | 0.48 | 33.5 | triangular | 26.535 | 19.784 | 6.973 | 0.6 |  |

Fig 10 The result of numerical modelling of the optimum sample

Fig 11 optimum sample before (A) and after (B) actuation

Conclusion

In this study, the input parameters affecting the performance of a morphing airfoil including the corrugation shape, pitch and thickness were optimized in order to have the lowest weight, maximum vertical displacement of the free end and morphing angle of 20 degrees. This was done using the RSM method in Design-Expert software and numerical modeling in order to measure the response of each designed experiment. Finally the optimum sample was chosen and analyzed further using the numerical and experimental procedure. The difference between the vertical displacement predicted by the numerical analysis and the measured value from the manufactured sample showed to be very negligible (1.42%), as a sign of promising model to be used for further investigations in this area in the future.

It was shown in this study that the combination of SMA and corrugated composite could be a suitable option for manufacturing of morphing airfoil. With the decrease in the pitch, a high displacement could be achievable in a corrugated structure while the increase in the morphing angle.

- References

Dayyani, I., et al., The mechanics of composite corrugated structures: a review with applications in morphing aircraft. Composite Structures, 2015. 133: p. 358-380.

Lloyd, P., Requirements for smart materials. Proceedings of the Institution of Mechanical Engineers, Part G: Journal of Aerospace Engineering, 2007. 221(4): p. 471-478.

Yokozeki, T., et al., Mechanical properties of corrugated composites for candidate materials of flexible wing structures. Composites Part A: applied science and manufacturing, 2006. 37(10): p. 1578-1586.

Kress, G. and M. Winkler, Corrugated laminate homogenization model. Composite Structures, 2010. 92(3): p. 795-810.

Thill, C., et al. Corrugated composite structures for aircraft morphing skin applications. in 18th international conference of adaptive structures and technologies. 2007. Citeseer.

Dayyani, I., S. Ziaei-Rad, and H. Salehi, Numerical and experimental investigations on mechanical behavior of composite corrugated core. Applied Composite Materials, 2012. 19(3-4): p. 705-721.

Ghabezi, P. and M. Golzar, Mechanical analysis of trapezoidal corrugated composite skins. Applied Composite Materials, 2013. 20(4): p. 341-353.

Golzar, M. and P. Ghabezi, Corrugated composite skins. Mechanics of Composite Materials, 2014. 50(2): p. 137-148.

Thill, C., et al., Composite corrugated structures for morphing wing skin applications. Smart Materials and Structures, 2010. 19(12): p. 124009.

Ge, R., et al., Deformation characteristics of corrugated composites for morphing wings. Frontiers of Mechanical Engineering in China, 2010. 5(1): p. 73-78.

Yokozeki, T., A. Sugiura, and Y. Hirano. Development and wind tunnel test of variable camber morphing wing. in 22nd AIAA/ASME/AHS adaptive structures conference. 2014.

Dayyani, I., et al., The design of a coated composite corrugated skin for the camber morphing airfoil. Journal of Intelligent Material Systems and Structures, 2015. 26(13): p. 1592-1608.

Ansari, M., M. Golzar, and A.H. Behravesh, Evaluation of corrugated composite beam deflection by shape memory alloy wire. Modares Mechanical Engineering, 2014. 14(8).

Talebi, H., et al. Nonlinear analysis of a corrugate composite panel actuated by shape memory alloy wire. in 22nd annual international conference on mechanical engineering, ISME2014-2185, Ahvaz, Iran. 2014.

Koudzari, M., M.-R. Zakerzadeh, and M. Baghani, Corrugated structures reinforced by shape memory alloy sheets: Analytical modeling and finite element modeling. Proceedings of the Institution of Mechanical Engineers, Part G: Journal of Aerospace Engineering, 2018

Sun G, Sun S, Wu X, Wu J. A study on thermomechanical deformation of elastic beam with embedded shape memory alloy wires. Materials & Design. 2000. 21(6): p. 525-8.

Baz A, Chen T, Ro J. Shape control of NITINOL-reinforced composite beams. Composites Part B: Engineering. 2000. 31(8): p. 631-42.

Zhou G, Lloyd P. Design, manufacture and evaluation of bending behaviour of composite beams embedded with SMA wires. Composites Science and Technology. 2009. 69(13): p. 2034-41.

Chaudhry, Z. and C.A. Rogers, Bending and shape control of beams using SMA actuators. Journal of Intelligent Material Systems and Structures, 1991. 2(4): p. 581-602.

Moallem, M., Deflection control of a flexible beam using shape memory alloy actuators. Smart Materials and Structures, 2003. 12(6): p. 1023.

Da Silva, E., Beam shape feedback control by means of a shape memory actuator. Materials & design, 2007. 28(5): p. 1592-1596.

Telford, J.K., A brief introduction to design of experiments. Johns Hopkins apl technical digest, 2007. 27(3): p. 224-232.

Khuri, A.I. and S. Mukhopadhyay, Response surface methodology. Wiley Interdisciplinary Reviews: Computational Statistics, 2010. 2(2): p. 128-149.

Ahaus, L., An airloads theory for morphing airfoils in dynamic stall with experimental correlation. 2010.

Anderson, J.D., Aircraft performance and design. 1999: WCB/McGraw-Hill.